## Slide 1
https://ogawalabteamsurface.dentistry.ucla.edu/
https://weintraubcenter.dentistry.ucla.edu/ogawa-lab-team-surface
Takahiro Ogawa, DDS, PhD
UCLA TEAM SURFACE
Professor, UCLA School of Dentistry
https://weintraubcenter.dentistry.ucla.edu/takahiro-ogawa
https://dentistry.ucla.edu/profile/ogawa-takahiro

## Slide 2
A new norm of implant science
Takahiro Ogawa, DDS, PhD
Professor
Prosthodontics and Weintraub Center
UCLA School of Dentistry
O2
O(1D)
O3
Singlet atomic oxygen
H2O
.OH
e-
h+
O2
.O2-
Superoxide anion
Hydroxyl radical
Implant pellicle and VUV
The Next Gen Implant Dentistry with VUV
Tak Ogawa

## Slide 3
Titanium undergoes biological aging.
1. Time-dependent hydrocarbon deposition on its surface
New
3-day old
7-day old
2-week old
1-month old
Unknown age

## Slide 4
Titanium undergoes biological aging.
Chart: 
 | 14 | 22 | 47 | 62
Day 0
Day 3
Week 2
Week 4
Surface carbonization (%)
14
62
22
47
Age of titanium

## Slide 5
The Next Gen Implant Dentistry with VUV
Titanium implant surfaces are no longer titanium.
Implant
pellicle
The hydrocarbon layer is defined as
The Next Gen Implant Dentistry with VUV
Tak Ogawa

## Slide 6
Implant pellicle vs dental pellicle
Implant
pellicle
The glycoproteins in the pellicle prevents continuous deposition of salivary calcium phosphate and, instead, attracts bacteria and bacterial products.
The dental pellicle is a protein film that forms on enamel, dentin, and crown surfaces by selective binding of glycoproteins from saliva.
The hydrocarbons in the pellicle prevents bone deposition and, instead, attracts bacteria and facilitates biofilm formation.
The implant pellicle is a carbon film that forms on implant surfaces by naural binding of hydrocarbons from atmosphere.

## Slide 7
Titanium undergoes biological aging.
New
1-day old
1-week old
3-month old
Hydrophilic
Hydrophobic
2. Time-dependent degradation of hydrophilicity

## Slide 8
Due to Ti aging,
4-week old implant
New implant
Bone-implant contact is compromised by 60%.
Strength of osseointegration is compromised by 55%.
The number of osteogenic cells attached to implants is compromised by 65%.
The amount of proteins adsorbed to implants is compromised by 75%.
Dental implants are severely bio-compromised.

## Slide 9
Titanium undergoes biological aging.
No exception

## Slide 10
A simple, reasonable idea.
Bring back titanium surfaces as they are meant to be.
Pellicle-free implants

## Slide 11
UV treatment restores bio-compromised titanium.
1. UV decarbonizes titanium surfaces and removes the implant pellicle.
Day 0
Day 3
Week 2
Week 4
Surface carbon (%)
Chart: 
 | 14 | 22 | 47 | 62
UV
14
14
62
22
47
Age of titanium

## Slide 12
Ti aging (Carbonization)
VUV (Decarbonization)
Pellicle-free implant surface
The Next Gen Implant Dentistry with VUV
Tak Ogawa

## Slide 13
UV treatment restores bio-compromised titanium.
2. Hydrophilicity simply follows the pellicle removal.
Before
After
Hydrophilic
Hydrophobic

## Slide 14
UV treatment restores bio-compromised titanium.
50 mm
UV-treated implant
Control implant
UV treatment of titanium accomplishes:
Near perfect bone-implant contact of 98.2%.
3-times faster osseointegration in early healing stage.
5-time greater protein adsorption to implant surface.
3- to 4-time greater number of osteogenic cells attached to implant surface at the initial stage.
UV treatment fully restores the compromised implants and even make them greater than the original new. This regeneration process is called UV-photofunctionalization or UV activation.

## Slide 15
VUV technology makes photofunctionalization to happen in 1 minute.
Xenon excimer vacuum UV (VUV)
172 nm wavelength
DIO Implant and UCLA have co-developed the next-generation UV technology called VUV-powered activation. By exploiting a cutting-edge vacuum, UV (VUV) light with a 172 nm wavelength combined with an innovative synthetic quartz technology — dental implants can now be activated in just one minute, without unpacking the implant.
Tak Ogawa

## Slide 16
VUV technology makes photofunctionalization to happen in 1 minute.
Decarbonizing
capability
VUV overwhelms other UV light sources and devices in decarbonizing capability.
The results of 1-minute decomposing of methylene blue (C16H18ClN3S) are shown.
UVC
HUVC
PUV
VUV

## Slide 17
Perfection finally surfaced.
The Dawn of a New Norm
The next generation implant dentistry
with VUV technology
VUV-activated, pellicle-free implant
Bio-compromised,
pellicled implant
Blood and cells can see the pellicle and react accordingly.
It is only natural we get rid of the pellicle.